Facile Synthesis of Zr-doped SrO₂ Nanomaterials for Sensitive Histidine Detection via Electrochemical Analysis

Mylarappa M1*, N Raghavendra2*, Shravana Kumar K N3, Chandruavasan S4

1Department of Studies in Chemistry, Bangalore University, Bengaluru-560056, Karnataka, India.

2Research Centre, Department of Chemistry, East West Institute of Technology, Bengaluru 560091, Karnataka, India.

3Department of Chemistry, GM University, Davangere, Karnataka, India.

4Department of Chemistry, KSOU, Mukhtagangotri, Mysore, 570006, Karnataka, India.

Corresponding authors: nraghavendra09@gmail.com,  mylu4mkallihatti@gmail.com

Abstract

This study describes the preparation of strontium oxide (SrO₂) and zirconium-doped SrO₂ (Zr–SrO₂) nanoparticles via a low-temperature solution combustion method using tannic acid. The study carefully examined the structure and shape of materials produced by different methods, including X-ray diffraction (XRD), energy-dispersive X-ray spectroscopy (EDX), and UV-visible spectroscopy (UV-Vis). The XRD shows that only one orthorhombic SrO₂ phase was formed, and that when Zr was added, the peaks became broader and the structure changed, indicating that Zr was incorporated. The analysis of crystallite size  showed that it changed from 21.7–31.1 nm (SrO₂) to 16.3–21.6 nm (Zr–SrO₂). This  change was because the dopant made the grains finer. Electrochemical tests with a Zr–SrO₂ electrode in a 2 M KOH solution showed that Zr–SrO₂ had much better redox activity and electrochemical activity via cyclic voltammetry (CV). Also, the Zr-doped sample showed a strong preference for histidine, indicating it might be helpful in creating biosensors. These results underscore the effectiveness of Zr doping in modulating the physicochemical and electrochemical behaviors of SrO2, making it a promising candidate for advanced electrochemical and biosensing applications.

Keywords: SrO₂, Zr-SrO₂, combustion process, electrochemical, biosensing.

1. Introduction

Nanotechnology has emerged as a transformative field of science, offering novel materials and devices at the nanoscale with superior performance compared to their bulk counterparts. Among these innovations, nanoparticles (NPs) have garnered significant interest due to their unique size-dependent properties and extensive applicability in various sectors such as electronics, energy, environment, biomedicine, food packaging, and cosmetics [1–3]. Inorganic nanoparticles, particularly metal oxides, are especially attractive due to their robust physicochemical properties, including large surface area-to-volume ratio, chemical stability, high thermal conductivity, mechanical strength, and multifunctionality [4–5]. These characteristics enable their use in catalysis, photovoltaics, sensors, drug delivery, and energy storage devices.

Recently, metal oxide nanoparticles (MONPs) have received attention for their promising role in next-generation supercapacitors (E-SCs), biosensors, and photochemical applications [6–8]. Their ability to exhibit multiple oxidation states enables reversible redox behavior, which is fundamental for charge-storage and energy-conversion applications [9]. Among these materials, SrO₂ has shown considerable potential due to its stable crystal structure, moderate band gap, and favorable redox chemistry [10].

SrO₂ nanoparticles have been explored for numerous applications such as catalysis [11], solar cells [12], fuel cells [13], and biomedical engineering [14]. Their pseudocapacitive nature, arising from their rich surface chemistry and the multivalence of Sr, makes them suitable candidates for energy storage devices [15]. Furthermore, SrO₂ exhibits photochemical activity that is vital for photocatalysis and environmental remediation [16]. Recent research has also explored its use in biomedicine, especially in dental applications, bone tissue engineering, and as an antibacterial agent [17].

Transition-metal doping has been a well-established strategy for tailoring the electrical and optical properties of metal oxides. Doping SrO₂ with transition metals such as Co²⁺, Ni²⁺, and Mn²⁺ has demonstrated improvements in charge-carrier mobility, catalytic activity, and electrochemical performance [18–19]. Notably, zirconium (Zr⁴⁺) has emerged as a particularly effective dopant due to its high charge-to-radius ratio and ability to integrate into oxide lattices without causing phase separation or instability [20]. Zr doping has been reported to enhance optical transparency, phase stability, and photocatalytic efficiency in various oxides, including TiO₂, ZnO, and SnO₂ [21–23].

In the case of SrO₂, Zr doping can refine the crystalline structure, improve electronic conductivity, and tailor the band gap to better match the desired electrochemical or optical response [24]. For example, the comparative electrochemical and sensing performance of SrO₂ and doped SrO₂-based materials is reported as shown in Table 1, which is advantageous for solar and sensor devices [25]. Moreover, Zr⁴⁺ incorporation can delay grain coarsening during annealing and help maintain anatase phase stability, contributing to higher surface areas and better sensing capability [26].

Electrochemical biosensing is another key application area for doped MONPs. Metal oxides such as Co₃O₄, NiO, and Fe₃O₄ are already employed as sensing platforms due to their ability to facilitate electron transport and amplify the redox signal [27–28]. In biosensing applications, nanomaterials offer improved electron transfer kinetics, enhanced catalytic activity, and resistance to surface fouling [29]. SrO₂, with its biocompatible and tunable redox properties, is increasingly studied for biosensing purposes [30]. When combined with Zr⁴⁺, the resultant nanostructure can potentially exhibit higher electrochemical sensitivity and selectivity toward biologically relevant analytes, such as amino acids and neurotransmitters [31].

Despite the expanding literature on metal oxide nanomaterials, a limited number of studies have systematically investigated the effect of Zr⁴⁺ doping on the electrochemical and biosensing performance of strontium oxide nanoparticles. Most prior research has focused on Zr doping in materials like TiO₂ and ZnO, with little emphasis on SrO₂-based systems [32–33]. Furthermore, few reports exist on the low-temperature synthesis of Zr-SrO₂ using energy-efficient routes, such as the solution combustion method, which offers advantages such as reduced reaction time, minimal energy input, and scalability [34]. Additionally, the biosensing applications of SrO₂, especially for detecting biologically important molecules such as histidine, an essential amino acid involved in metal chelation and enzyme function, are relatively unexplored [35]. There exists a knowledge gap in understanding how Zr incorporation affects the electrochemical properties and redox response of SrO₂, which is key to maximizing its performance in biosensor devices.

To address these gaps, the present study focuses on the synthesis of SrO₂ and Zr-SrO₂ nanoparticles via a low-temperature solution combustion technique, followed by comprehensive characterization. Structural and optical features were studied by XRD and UV-visible spectroscopy, while electrochemical behavior was examined by CV. The redox characteristics and sensing abilities of these materials for histidine detection were evaluated, highlighting the influence of Zr doping on sensor performance. This research offers previously unknown information about the design of efficient, low-cost, and scalable nanomaterials for biosensor applications.

Table 1.  Comparison of the electrochemical and sensing abilities of SrO₂ and other materials.

| Material | Dopant Type | Key Properties | Electrochemical / Sensing Performance | Key Advantage | Ref. |
| --- | --- | --- | --- | --- | --- |
| SrO₂ (pristine) | — | Stable crystal structure, moderate band gap, intrinsic redox activity | Moderate pseudocapacitive behavior; limited conductivity | Baseline material with good chemical stability | [10], [15], [30] |
| Co-doped SrO₂ | Co²⁺ | Enhanced charge carrier density and catalytic sites | Improved redox kinetics and current response | Better catalytic and electrochemical activity | [18] |
| Ni-doped SrO₂ | Ni²⁺ | Increased electrical conductivity and surface activity | Enhanced charge transfer and sensing response | Improved electron transport properties | [18–19] |
| Mn-doped SrO₂ | Mn²⁺ | Multiple oxidation states contribute to redox reactions | Improved pseudocapacitive performance | Higher redox reversibility | [19] |
| Zr-doped SrO₂ (this work) | Zr⁴⁺ | High charge-to-radius ratio, lattice stabilization, oxygen vacancies | Significantly enhanced peak current, improved reversibility, and faster electron transfer kinetics | Superior sensitivity and electrochemical performance due to defect engineering | [20], [24]; this work |
| Zr-doped TiO₂ | Zr⁴⁺ | Improved phase stability and surface area | Enhanced photocatalytic and electrochemical activity | High stability and efficient charge separation | [21] |
| Zr-doped ZnO | Zr⁴⁺ | Tunable band gap and improved conductivity | Improved sensing and catalytic efficiency | Better optical and electrical properties | [22] |
| Zr-doped SnO₂ | Zr⁴⁺ | Increased oxygen vacancies and surface defects | Enhanced gas sensing and electrochemical response | High sensitivity and selectivity | [23] |
| Zr-doped SrTiO₃ | Zr⁴⁺ | Improved ferroelectric and photoelectrochemical properties | Enhanced photocurrent and sensing performance | Better charge separation and stability | [25] |

2. Materials and Methods

2.1 Chemicals and Reagents

Strontium nitrate [Sr(NO₃)₂], zirconium nitrate [Zr(NO₃)₄], and tannic acid (C₇₆H₅₂O₄₆) were used as starting materials. All chemicals were of analytical grade and procured from standard commercial suppliers without any further purification. Distilled water was used as the solvent throughout the synthesis process. Tannic acid served both as a fuel and a green reducing agent in the combustion reaction.

2.2 Synthesis of SrO₂

SrO₂ nanoparticles were synthesized via a low-temperature solution combustion method. Precisely 1.242 g of Sr(NO₃)₂ and 1.0 g of tannic acid were dissolved in a minimal amount of distilled water under continuous stirring to form a homogeneous solution. The resulting mixture was transferred into a ceramic crucible and placed in a preheated muffle furnace maintained at 500 °C. Upon heating, the solution underwent dehydration and decomposition, releasing gaseous by-products. At a critical temperature, spontaneous ignition occurred, and a self-sustaining combustion reaction ensued. This highly exothermic process lasted for approximately 5 minutes, resulting in the rapid formation of a dry, foamy residue. The greyish-black product, presumed to be SrO₂, was allowed to cool to room temperature, then finely ground using an agate mortar and pestle and stored in an airtight container for subsequent analysis.

2.3 Synthesis of Zr-SrO₂

For the synthesis of Zr-SrO₂ nanoparticles, 1.242 g of Sr(NO₃)₂, 1.465 g of Zr(NO₃)₄, and 2.0 g of tannic acid were dissolved in distilled water with constant stirring until a clear solution was obtained. The prepared solution was poured into a crucible and introduced into a muffle furnace preheated to 500 °C. As with the SrO₂ synthesis, the solution underwent a sequence of boiling, dehydration, and thermal decomposition steps. The combustion reaction was spontaneously triggered at the ignition temperature, resulting in a rapid exothermic reaction that completed within 5 minutes. The resulting black powder, attributed to Zr-doped SrO₂, was cooled, ground into a uniform fine powder, and stored for further characterization.

2.4 Working electrode preparation

Working electrodes were fabricated by mixing 0.25 g of the synthesized active material with 0.2 g of graphite and 3–5 drops of polytetrafluoroethylene (PTFE) binder to form a homogenous paste. This mixture was uniformly coated onto a nickel mesh (area = 1 cm²) and allowed to dry under ambient conditions. Electrochemical measurements were performed in a typical three-electrode system, using the prepared electrode as the working electrode, a platinum wire as the counter electrode, and an Ag/AgCl reference electrode in 2 M KOH aqueous electrolyte.

2.5 Characterization Techniques

The synthesis of SrO₂ and Zr-SrO₂ nanoparticles was examined using an XRD Maxima-7000 instrument from Shimadzu to analyze their structural features. Morphology and EDX analyses were performed with a JEOL JSM-5600LV and a SU-1500 from HITACHI. The UV-Vis absorption spectrum was obtained using an SL 159 ELICO UV-Visible spectrophotometer. Electrochemical activity was assessed using an ACHI608E potentiostat in a three-electrode setup, with a modified electrode, a platinum wire, and Ag/AgCl as the working, counter, and reference electrodes, respectively. A 0.1 M HCl solution served as the electrolyte.

3. Results and discussion

3.1 XRD studies

The structural properties of the synthesized SrO₂ and Zr–SrO₂ nanoparticles were investigated using powder XRD, as shown in Figs. 1a and 1b. The analysis offers important details about the phase composition, crystallinity, and the influence of Zr⁴⁺ substitution on the SrO₂ crystal lattice, which are discussed.  This study examines the influence of Zr⁴⁺ substitution on the SrO₂ crystal lattice. The XRD pattern of pure SrO₂ (Fig. 1a) exhibits sharp and intense peaks at 2θ values of 22.8°, 26.6°, 29.7°, 32.1°, 39.5°, 46.5°, 52.7°, 57.4°, 62.6°, and 68.5°, which correspond to the crystal planes (100), (110), (200), (111), (200), (210), (211), (220), and (221), respectively. These reflections are consistent with the standard JCPDS card for orthorhombic SrO₂, confirming the formation of a single-phase orthorhombic structure with high crystallinity [36]. The most intense peak at 22.8° (assigned to the (100) plane) indicates a preferred growth orientation along this plane. The narrow full width at half maximum (FWHM) of the peaks suggests that SrO₂ particles have larger crystallite sizes and minimal microstrain, indicative of well-developed crystalline domains.

In the case of Zr-SrO₂ (Fig. 1b), the XRD pattern retains the fundamental peaks of SrO₂, indicating the preservation of the orthorhombic crystal structure even after Zr incorporation. There is, however, significant peak broadening and minor changes to elevated 2θ angles, particularly everywhere. ever. Significant peak broadening and minor changes to elevated 2θ angles are apparent, especially around the (100), (110), and (200) planes. These changes are attributed to the substitution of Sr²⁺ (ionic radius 1.18 Å) by the smaller Zr⁴⁺ ions (ionic radius 0.72 Å) [37, 38], which introduce compressive strain and lattice distortion into the crystal matrix.  Additionally, a modest reduction in the relative peak intensities for Zr-SrO₂ suggests defect formation or decreased ordering due to dopant-induced strain.  The lack of secondary peaks in both patterns confirms that the samples are single-phase and supports the idea that Zr can form a solid solution within the SrO₂ lattice.

To quantify the influence of doping on the crystallite size, the average crystallite dimensions were estimated using the Debye–Scherrer equation. A comparison of peak positions, Miller indices, and calculated crystallite sizes is provided in Table 2.

Fig 1.  The XRD patterns of (a) SrO₂ and (b) Zr-SrO₂ are shown.

Table 2.  XRD peak positions, Miller indices, and calculated crystallite sizes for SrO₂ and Zr–SrO₂.

| 2θ (°) | Miller Indices (hkl) | SrO₂ FWHM (β, rad) | D (SrO₂) (nm) | Zr–SrO₂ FWHM (β, rad) | D (Zr–SrO₂) (nm) |
| --- | --- | --- | --- | --- | --- |
| 22.8 | (100) | 0.0052 | 28.6 | 0.0078 | 19.1 |
| 26.6 | (110) | 0.0048 | 31.1 | 0.0069 | 21.6 |
| 29.7 | (200) | 0.0060 | 24.6 | 0.0083 | 17.8 |
| 32.1 | (111) | 0.0063 | 23.3 | 0.0086 | 17.1 |
| 39.5 | (200) | 0.0057 | 26.5 | 0.0080 | 18.8 |
| 46.5 | (210) | 0.0050 | 30.2 | 0.0074 | 20.1 |
| 52.7 | (211) | 0.0068 | 21.7 | 0.0091 | 16.3 |

3.2 SEM analysis

Fig. 2 presents the SEM micrographs of (a) SrO₂ and (b) Zr-doped SrO₂ (Zr–SrO₂) synthesized materials. These images reveal significant morphological changes resulting from Zr doping in the SrO₂ matrix. The SEM image of pristine SrO₂ (Fig. 2a) exhibits irregular, agglomerated particles with a rough surface texture. The particles are relatively large and unevenly distributed, showing a tendency to cluster into micron-sized aggregates. This morphology is characteristic of oxide materials synthesized via combustion or precipitation methods, where rapid reaction kinetics often lead to uncontrolled grain growth and poor dispersion [39]. The loosely packed, porous structure of SrO₂ may mean that it has a small surface area, which could affect how well it works in applications like sensing or catalysis.

Notable changes in particle morphology occur upon incorporating Zr into the SrO₂ matrix (Fig. 2b). The Zr–SrO₂ sample displays a more refined microstructure, with reduced particle size and enhanced uniformity. The dispersion of particles appears significantly improved, and the agglomeration is comparatively less pronounced. The red-circled region highlights a layered or flake-like surface texture, likely resulting from structural distortion introduced by Zr doping. Furthermore, the area labelled “Zr” suggests localized Zr-rich domains or surface modifications associated with Zr integration that contribute to the observed microstructural refinement.

The morphological change that happens when Zr is added is because Zr⁴⁺ ions stop SrO₂ grains from growing during synthesis. Zirconium is known to act as a grain refiner, promoting homogeneous nucleation while suppressing particle coalescence and excessive crystallite growth, leading to enhanced textural properties and increased active surface area [40]. Such morphological characteristics are often beneficial in materials intended for heterogeneous catalysis, electrochemical sensing, or solid-state devices, where surface activity and uniformity are key variables that determine functional efficiency.

a) SrO2

a) Zr-SrO2

Zr

The SEM analysis demonstrates the impact of Zr doping on the microstructure of SrO₂. While pristine SrO₂ shows large, agglomerated particles with uneven distribution, Zr–SrO₂ exhibits a more homogeneously dispersed, fine-grained morphology. These results suggest that Zr incorporation improves the structural properties of SrO₂, potentially enhancing its performance in various functional applications.

Fig. 2. SEM micrographs of (a) SrO2 and (b) Zr-SrO₂.

3.3 EDX studies

The elemental composition of SrO₂ and Zr–SrO₂ nanoparticles was examined using EDX, as shown in Figs. 3(a) and 3(b). The EDX spectrum of pristine SrO₂ exhibits characteristic peaks corresponding to Sr and O, confirming the formation of strontium oxide without detectable impurity phases. A minor carbon signal is observed, which can be attributed to surface contamination or the carbon tape used during sample preparation. The presence of a small Au peak is associated with the gold coating applied to improve conductivity during SEM analysis.

a)

b)

Fig. 3 EDX spectrum of (a) SrO2 and (b) Zr-SrO₂.

In the case of Zr–SrO₂, additional peaks corresponding to Zr are clearly observed along with Sr and O, confirming the successful incorporation of zirconium into the SrO₂ matrix. No secondary elemental peaks were detected, indicating high chemical purity and the absence of unwanted phases. The compositional results are consistent with XRD findings and verify that Zr doping was achieved without altering the overall phase purity of the host lattice. The confirmed elemental incorporation supports the enhanced structural and electrochemical properties observed for the doped sample.

3.4 UV-visible spectroscopy studies

Fig. 4 illustrates the optical absorption behavior and estimated band gap energies of (a) SrO₂ and (b) Zr–SrO₂ based on UV–Vis diffuse reflectance spectroscopy (DRS) data. The inset in both graphs represents the absorbance vs. wavelength curves, while the main graphs show Tauc’s plots, constructed to determine the optical band gap energy. The UV–vis absorbance spectrum of pristine SrO₂ (inset of Fig. 4a) reveals a moderate absorption in the UV region (200–900 nm), with a steep onset of absorption, suggesting that it is a semiconductor with a wide band gap.

The corresponding Tauc’s plot, drawn using the Kubelka–Munk function and assuming an indirect allowed transition, (αhv)² vs. hv, displays a linear region extrapolated to the energy axis to estimate the optical band gap. The calculated band gap for SrO₂ is approximately 3.47 eV, consistent with previous reports for alkaline earth metal oxides possessing wide band gaps [41]. This wide band gap implies that SrO₂ is optically transparent in the visible region, which can be advantageous in optoelectronic, photocatalytic, and UV shielding applications [42].

However, such a wide band gap may limit its photocatalytic efficiency under visible light unless modified via doping or surface engineering. Upon doping with Zr, the optical properties of the material exhibit notable changes, as shown in Fig. 4b. The UV–vis absorbance spectrum (inset) of Zr–SrO₂ shows an enhanced absorption tail extending into the visible region, indicating the generation of sub-bandgap states or a narrowing of the band gap. The corresponding Tauc’s plot shows a reduced band gap energy of 3.2 eV. The decrease in band gap upon Zr doping may be attributed to lattice distortion and the introduction of defect states or oxygen vacancies, which allow electronic transitions at lower photon energies [43]. Such band gap engineering enhances the potential applicability of Zr–SrO₂ in photocatalytic degradation, photoelectrochemical water splitting, and light-assisted sensing.

Fig. 4. The UV-Vis and Tauc’s plot of (a) SrO2 and (b) Zr-SrO₂.

3.5 Electrochemical studies

3.5.1 CV studies

The electrochemical behavior, proton diffusion efficiency, and energy storage capability of SrO₂ and Zr–SrO₂ were evaluated using CV and are presented in Fig. 5(a–d). The CV measurements were carried out within a potential window of −1.0 to +1.0 V at scan rates ranging from 10 to 100 mV/s. Fig. 5 (a, c) shows the CV behavior of SrO₂ and Zr–SrO₂. The strong redox features are due to the fact that zirconium is electroactive in the host lattice. behavior of SrO₂ and Zr–SrO₂, where the pronounced redox features can be attributed to the electroactive role of zirconium within the host lattice. The incorporation of Zr⁴⁺ ions into the SrO₂ matrix induces lattice distortion and creates additional defect sites, particularly oxygen vacancies, which facilitate enhanced charge transfer kinetics. The observed cathodic and anodic peaks correspond to the reversible redox transition between Zr⁴⁺/Zr³⁺ states, indicating the active participation of zirconium in the electron transfer process. Compared to pristine SrO₂, the Zr–SrO₂ electrode exhibits higher peak currents and improved peak definition, suggesting increased electrochemical activity and conductivity. Furthermore, the systematic increase in peak current with scan rate confirms a diffusion-controlled redox mechanism, while the slight shift in peak potential indicates quasi-reversible behavior. The strong interaction between Zr ions and the SrO₂ lattice enhances electron mobility and provides additional active sites, thereby improving the overall redox performance. This enhanced electrochemical behavior highlights the significant role of Zr doping in tuning the redox properties of SrO₂, making it a promising candidate for high-performance electrochemical sensing applications. The closer spacing of the oxidation (EO) and reduction (ER) peaks indicates better electron movement in Zr–SrO₂ [44].

The proton diffusion coefficient (D) was estimated from the scan rate-dependent CV data, as shown in Fig. 5 (b, d). The calculated D values were 0.16 cm²/s for SrO₂ and 0.26 cm²/s for Zr–SrO₂, indicating that Zr doping significantly enhances ion diffusion and charge transport within the electrode matrix (Table 3 and Table 4). A higher diffusion coefficient, coupled with improved redox reversibility, clearly demonstrates the superior electrochemical kinetics of the Zr–SrO₂ system [45].

In addition to electrochemical reversibility and ion transport, the specific capacitance (Cₛₚ) of the electrodes was calculated using the following Eq. (1):

Csp=A2msV2-V1…………. (1)

where A - area under the CV curve, m - mass of active material, s - scan rate, and V₂ – V₁ - potential window.

This parameter quantifies the electrode material's energy storage capacity. The specific capacitance was found to be approximately 72.68 F/g for SrO₂ and significantly enhanced to 201.99 F/g for Zr–SrO₂. The more than two-fold increase in capacitance is attributed to increased surface area, improved electronic conductivity, and higher density of electroactive sites resulting from Zr doping [46]. The electrochemical analysis demonstrates that Zr doping in SrO₂ significantly improves its redox reversibility, enhances proton diffusion, and markedly increases its energy storage capability. These enhancements render Zr–SrO₂ a promising candidate for applications in electrochemical sensors, supercapacitors, and bio-electronic interfaces.

Fig. 5. CV curves (a, c) and Sq., the square root of scan rate (mV/s) (b, d) of SrO₂ and Zr-SrO₂.

Table 3. Reversibility and proton diffusion coefficient of SrO2.

| Scan Rate | E0 x 10-3 | -ER x 10-3 | E0 – ER x 10-3 | D x 10-3 | Csp |
| --- | --- | --- | --- | --- | --- |
| 10 | 1.65 | 1.677 | 3.327 | 0.265 | 72.68 |
| 20 | 2.05 | 2.375 | 4.425 |  |  |
| 30 | 2.3 | 2.451 | 4.751 |  |  |
| 40 | 2.517 | 2.892 | 5.409 |  |  |
| 50 | 2.73 | 3.213 | 5.943 |  |  |
| 60 | 2.94 | 3.455 | 6.395 |  |  |
| 70 | 3.12 | 3.721 | 6.841 |  |  |
| 80 | 3.27 | 3.94 | 7.21 |  |  |
| 90 | 3.411 | 4.134 | 7.545 |  |  |
| 100 | 3.525 | 4.328 | 7.853 |  |  |

Table 4. Reversibility and proton diffusion coefficient of Zr-SrO2.

| Scan Rate | E0 x 10-3 | -ER x 10-3 | E0 – ER x 10-3 | D x 10-3 | Csp |
| --- | --- | --- | --- | --- | --- |
| 10 | 1.26 | 4.915 | 6.175 | 0.168 | 201.99 |
| 20 | 1.45 | 6.019 | 7.469 |  |  |
| 30 | 1.6 | 6.763 | 8.363 |  |  |
| 40 | 1.73 | 7.314 | 9.044 |  |  |
| 50 | 1.87 | 7.746 | 9.616 |  |  |
| 60 | 1.972 | 8.162 | 10.134 |  |  |
| 70 | 2.088 | 8.331 | 10.419 |  |  |
| 80 | 2.182 | 8.482 | 10.664 |  |  |
| 90 | 2.261 | 8.824 | 11.085 |  |  |
| 100 | 2.35 | 8.798 | 11.148 |  |  |

3.5.2 Electrochemical biosensing of histidine using SrO₂ and Zr–SrO₂ electrodes.

The histidine-sensing behavior of the synthesized SrO₂ and Zr–SrO₂ materials was investigated using CV and is presented in Fig. 6(a, b). The measurements were carried out at varying histidine concentrations (1–8 mM) with a scan rate of 30 mV (2 M KOH) to evaluate the electrochemical response, sensitivity, and redox behavior of both sensing platforms. Histidine is an essential amino acid with biological significance, and its electrochemical detection is of growing interest for biosensing, medical diagnostics, and food quality monitoring [47].

In Fig. 6a, the SrO₂ electrode exhibits a pair of redox peaks in response to histidine addition within the potential window. As the histidine concentration increases from 1 to 8 mM, both the anodic and cathodic peak currents increase, indicating that the redox reaction is concentration-dependent. This current enhancement suggests an efficient electrocatalytic interaction between SrO₂ and histidine, enabling effective electron transfer and signal amplification [48]. However, the peak separation remains relatively broad, and the redox features are less defined, which may be attributed to the limited conductivity and slower electron mobility of pristine SrO₂. Additionally, the relatively lower peak currents at higher concentrations suggest that the SrO₂-based sensor may have moderate sensitivity to histidine.

Fig. 6b shows the corresponding CV curves for the Zr–SrO₂ electrode under the same histidine concentrations. A marked improvement in the current response is observed when compared to SrO₂. The anodic peak currents increase significantly with histidine concentration, and the redox peaks appear sharper and more symmetric, indicating better electrochemical reversibility and faster charge transfer kinetics. The distinct separation of peaks and higher signal amplitude even at lower concentrations implies that the Zr–SrO₂ electrode has a higher sensitivity and electrocatalytic activity toward histidine oxidation. These results strongly support that Zr doping facilitates better charge transfer and adsorption kinetics, improving histidine oxidation and overall sensor performance [49].

The electrochemical sensing data confirm that Zr–SrO₂ exhibits superior electrocatalytic properties and higher sensitivity toward histidine detection compared to pristine SrO₂.  The improved performance is due to the combined effects of zirconium doping, which makes conductivity, active surface sites, and redox reversibility better. These findings demonstrate the potential of Zr-SrO₂-based materials for amino acid biosensing applications in biomedical and environmental analysis.

Fig. 6. (a, b) CV response of SrO2 and Zr-SrO2 using histidine sensors.

4. Conclusion

In this study, SrO₂ and Zr–SrO₂ nanoparticles were successfully synthesized via a low-temperature combustion route, and their structural characteristics were thoroughly investigated using XRD. The analysis confirmed the formation of a single-phase orthorhombic crystal structure for both SrO₂ and Zr–SrO₂, with no detectable secondary phases, affirming the structural stability of the host lattice upon Zr doping.

The pristine SrO₂ sample exhibited sharp and intense diffraction peaks, indicative of high crystallinity and large crystallite size. Upon doping with zirconium, notable changes were observed in the XRD patterns, including peak broadening, reduced intensity, and minor shifts toward higher 2θ values. These variations are attributed to the incorporation of smaller Zr⁴⁺ ions into the SrO₂ lattice, which induced lattice distortion, compressive strain, and microstructural defects.

Crystallite size calculations based on the Debye–Scherrer equation revealed a clear reduction in average crystallite dimensions, from approximately 21.7–31.1 nm for SrO₂ to 16.3–21.6 nm for Zr–SrO₂. This reduction suggests that Zr doping effectively inhibited crystal growth during  synthesis, leading to enhanced surface area and defect density factors that are highly beneficial for catalytic, electrochemical, and sensing applications.

Overall, the results confirm that Zr⁴⁺ doping modulates the structural properties of SrO₂ by refining the crystallite size and introducing a controlled lattice strain without disrupting phase integrity. We anticipate that these modifications will significantly influence the material's functional performance in applications such as energy storage, chemical sensing, and photocatalysis. Further investigations focusing on the electrochemical behavior and surface characteristics of these materials would reveal more about their practical utility in advanced technological applications.

Conflicts of Interest:

The authors declare no conflicts of interest.

Author Contributions:

M. M, N R.: Performed experiments, analysis, wrote the paper, and supervised the research; designed, performed experiments; analyzed data; and wrote the final manuscript and editing. S. K.K N, C. S: Analyzed data and co-wrote the paper.

Funding:

The authors received no financial support for the research, authorship, and/or publication of this article.

References

- Ibrahim Khan, Khalid Saeed, and Idrees Khan. Nanoparticles: Properties, applications and toxicities. Arabian Journal of Chemistry, 12(7), 908-931. doi: 10.1016/j.arabjc.2017.05.011

- Stefanos Mourdikoudis, Roger M. Pallares, and Nguyen T. K. Thanh. Characterization techniques for nanoparticles: comparison and complementarity upon studying nanoparticle properties, Nanoscale, 2018, 10, 12871–12934.

- K.A. Altammar, A review on nanoparticles: characteristics, Synthesis, applications, and challenges. Frontiers in Microbiology, 17(14), 2023, 115562. doi: 10.3389/fmicb.2023.1155622.

- G. Unnikrishnan, A. Joy, M. Megha, Elayaraja Kolanthai, M. Senthilkumar, Exploration of inorganic nanoparticles for revolutionary drug delivery applications: a critical review. Discover Nano, 18, 2023, 157. https://doi.org/10.1186/s11671-023-03943-0

- Y. Khan, H. Sadia, S.Z. Ali Shah, M.N. Khan, A.A. Shah, N. Ullah, M.F. Ullah, H. Bibi, O.T. Bafakeeh, N.B. Khedher, Classification, Synthetic, and Characterization Approaches to Nanoparticles, and Their Applications in Various Fields of Nanotechnology: A Review. Catalysts, 12(11), 2022, 1386. https://doi.org/10.3390/catal12111386

- Dadaso D. Mohite, Sachin S. Chavan, Prasad E. Lokhande, Kailasnath B. Sutar, Sumit Dubal, Udaybhaskar Rednam, Bandar Ali Al-Asbahi, Yedluri Anil Kumar, Metal oxide-based nanocomposites as advanced electrode materials for enhancing electrochemical performance of supercapacitors: A comprehensive review, Materials Today: Proceedings, 2024, ISSN 2214-7853, https://doi.org/10.1016/j.matpr.2024.05.001.

- P. Kannan, G. Maduraiveeran, Metal Oxides Nanomaterials and Nanocomposite-Based Electrochemical Sensors for Healthcare Applications. Biosensors. 13(5), 2023, 542. https://doi.org/10.3390/bios13050542

- Upendra Devendra Lad, Recent Advancement in Metal Oxides Based Supercapacitors and Future Perspectives: A Short Review. International Journal on Science and Technology. 16, 2025.  10.71097/IJSAT.v16.i3.8057.

- A. Das, S.D. Peu, M. S. Hossain, M.A.M. Akanda, M.M. Salah, M.M.H. Akanda, M. Rahman, B. K. Das. Metal Oxide Nanosheet: Synthesis Approaches and Applications in Energy Storage Devices (Batteries, Fuel Cells, and Supercapacitors). Nanomaterials, 13(6), 2023,1066. https://doi.org/10.3390/nano13061066

- H.S. Patel, V.A. Dabhi, A.M. Vora, Investigating Electronic, Optical, Thermodynamic, and Thermoelectric Properties of SrO and SrO2 Phases: A Density Functional Theory Approach. ACS Omega, 1;8(45), 2023, 43008-43023. doi: 10.1021/acsomega.3c06221.

- S. Kavitha, K.S. Mohan, K. Deepika, P.R. Janani, B. Kamali, S. Bhavadharani, The Impact of Zn doping on structural and optical behavior of SrO2 NPs and Anti-Microbial activities for Zn@SrO₂ NPs, Materials Today: Proceedings, 94, 2023, Pages 1-12, https://doi.org/10.1016/j.matpr.2023.04.331.

- K.B. Kusuma, M. Manju, C.R. Ravikumar, N. Raghavendra, T. Naveen Kumar, M.R. Anilkumar, H.P. Nagaswarupa, T.R. Shashi Shekhar, H.C. Ananda Murthy, K.U. Aravind, Synthesis of strontium oxide nanoparticles by probe sonication method: Its photocatalytic activity and electrochemical sensor studies, Sensors International, 4, 2023, 100231, https://doi.org/10.1016/j.sintl.2023.100231.

- Annin K. Shimi, C. Parvathiraj, Suman Kumari, Jasvir Dalal, Vipan Kumar,  Saikh M. Wabaidur, Zeid A. Alothman, Green Synthesis of SrO nanoparticles using leaf extract of Albizia julibrissin and its recyclable photocatalytic activity: an eco-friendly approach for treatment of industrial wastewater,
Environmental Science Advances, 1, 2022, 849-861. DOI https://doi.org/10.1039/D2VA00018K

- Efrat Ohayon Naor, Miri Koberg, Aharon Gedanken, Nonaqueous Synthesis of SrO nanopowder and SrO/SiO2 composite and their application for biodiesel production via microwave irradiation, Renewable Energy, 101, 2017, 493-499, https://doi.org/10.1016/j.renene.2016.09.007.

- Sohyun Jin, Haein Lee and Sanggyu Yim. Enhanced capacitive properties of all-metal-oxide-nanoparticle-based asymmetric supercapacitors, RSC Advances, 9, 2019, 31846-31852. DOI: 10.1039/C9RA06066A

- Dhakshnamoorthi Harikaran, Vijayaraghavan R, Strontium peroxide as a potential photocatalyst: rapid degradation of organic and pharmaceutical pollutants, New Journal of Chemistry, 47, 2023, 20733-20743. https://doi.org/10.1039/D3NJ03546H

- S. M. Mawazi, M. Kumar, N. Ahmad, Y. Ge, S. Mahmood, Recent Applications of Chitosan and Its Derivatives in Antibacterial, Anticancer, Wound Healing, and Tissue Engineering Fields. Polymers, 16(10), 2024, 1351. https://doi.org/10.3390/polym16101351

- A.J. Fernández-Ropero, J.M. Porras-Vázquez, A. Cabeza, P.R. Slater, D. Marrero-López, E.R. Losilla, High valence transition metal doped strontium ferrites for electrode materials in symmetrical SOFCs, Journal of Power Sources, 249, 2014, 405-413, https://doi.org/10.1016/j.jpowsour.2013.10.118.

- A. Yousfi, M. El Bouji, Y. Nejmi, Y. Ait-Alla, H. El Farri, N. Ait Labyad, I. Benaicha, A. El-Habib, A. Fahmi, A. Raidou, S. Amraoui, K. Nouneh, M. Taibi, M. Fahoume . Impact of transition metal doping on the optical and electrical properties of zinc sulfide: advancing photovoltaic performance. J Mater Sci: Mater Electron 36, 1845 (2025). https://doi.org/10.1007/s10854-025-15840-6

- A. Sanchez-Navasa, S. Melchorb, J. Ortega-Castroc, I. Vidal-Dazab, A. Castrod, A case study of depolymerization in silicates: Melting of quartz and zircon crystallization at high pressure Chemical Geology, 661, 2024, 122156.

- Ishchenko Olga, Roge Vincent, Lamblin Guillaume, Lenoble Damien, Fechete Ioana, TiO2, ZnO, and SnO2 -based metal oxides for photocatalytic applications: principles and development. Comptes Rendus. Chimie. 24, 2021, 10.5802/crchim.64.

- Mehrdad Mehdikhanloo, Zahra Hagheh Kavousi, Massomeh Ghorbanloo, Amr A. Nada, Heba H. El-Maghrabi, Rasha Hosny, Fouad Zahran, Roman Viter, Djamel Bezzerga, Jisang Hong, Bernard Fraisse, Fathi S. Soliman, Igor Iatsunskyi, Emerson Coy, Yaovi Holade, Mitra Saffari, Mikhael Bechelany, Influence of interface defects and Zr doping on the photocatalytic activity of TiO2 nanofibers in water splitting, Journal of Alloys and Compounds, 1020, 2025, 179439, https://doi.org/10.1016/j.jallcom.2025.179439.

- Ameer Baig Ali Baig, Vadamalar Rathinam, Jayanthi Palaninathan, Fabrication of Zr‑doped SnO2 nanoparticles with synergistic influence for improved visible‑light photocatalytic action and antibacterial performance, Applied Water Science, 10:54, 2020, https://doi.org/10.1007/s13201-019-1119-1

- D. Nematov, A. Burkhonzoda, K. Kholmurodov, A. Lyubchyk, S. Lyubchyk, S. Lyubchyk, Study on Structural Stability of ZrO2 and YSZ: Doping-Induced Phase Transitions and Fermi Level Shift. Preprints, 2023, 2023090350. https://doi.org/10.20944/preprints202309.0350.v1

- Shahran Ahmed, A.K.M. Sarwar Hossain Faysal, M.N.I. Khan, M.A. Basith, Muhammad Shahriar Bashar, H.N. Das, Tarique Hasan, Imtiaz Ahmed, Room temperature ferroic orders in Zr and (Zr, Ni) doped SrTiO3, Results in Physics, 31, 2021, 104940, https://doi.org/10.1016/j.rinp.2021.104940.

- Wang Yan, Liu Su, Lu Meng, Wang Shu, Gu Feng, Gai Xue, Cui Xiao, Pan Jie. Preparation and Photocatalytic Properties of Zr⁴⁺-Doped TiO₂ Nanocrystals.  Journal of Molecular Catalysis A-chemical, 215, 2004, 137-142. 10.1016/j.molcata.2004.01.007.

- Kannan P, Maduraiveeran G. Metal Oxides Nanomaterials and Nanocomposite-Based Electrochemical Sensors for Healthcare Applications. Biosensors. 13(5), 2023, 542. https://doi.org/10.3390/bios13050542.

- Sumit Malik, Joginder Singh, Rohit Goyat, Yajvinder Saharan, Vivek Chaudhry, Ahmad Umar, Ahmed A. Ibrahim, Sheikh Akbar, Sadia Ameen, Sotirios Baskoutas, Nanomaterials-based biosensor and their applications: A review, Heliyon, 9 (9), 2023, https://doi.org/10.1016/j.heliyon.2023.e19929.

- Chengzhou Zhu, Guohai Yang, He Li, Dan Du, Yuehe Lin, Electrochemical Sensors and Biosensors Based on Nanomaterials and Nanostructures, Anal. Chem. 2015, 87(1), 230–249, https://doi.org/10.1021/ac5039863.

- Harikaran, Dhakshnamoorthi, Vijayaraghavan, Rajagopalan. Strontium peroxide as a Potential Photocatalyst: Rapid Degradation of Organic and Pharmaceutical Pollutants. New Journal of Chemistry. 47, 2023, doi:10.1039/D3NJ03546H.

- Zhaowei Sun, Lei Wang, Shuai Wu, Yanhong Pan, Yu Dong, Sha Zhu, Jie Yang, Yongmei Yin, Genxi Li, An Electrochemical Biosensor Designed by Using Zr-Based Metal–Organic Frameworks for the Detection of Glioblastoma-Derived Exosomes with Practical Application, Analytical Chemistry 92(5), doi: 10.1021/acs.analchem.9b05241.

- Jafar Ali Ibrahim S, Rajasekar S, Varsha, Karunakaran M, Kasirajan K, Kalyan Chakravarthy N.S, Kumar V, and Kaur K.J. Recent advances in performance and effect of Zr doping with ZnO thin film sensor in ammonia vapour sensing, Global NEST Journal, 23(4), 526-531.

- Sharma, Jayanti, Gupta, Aayush, Pandey, O. Effect of Zr doping and aging on optical and photocatalytic properties of ZnS nanopowder. Ceramics International. 45. 2019.  10.1016/j.ceramint.2019.04.061.

- Nikita Sharma, P.P. Sahay, Solution combustion synthesis of Dy-doped ZnO nanoparticles: An investigation of their structural, optical and photoluminescence characteristics, Journal of Luminescence, 257, 2023, 119655, https://doi.org/10.1016/j.jlumin.2022.119655.

- Qian Zhang, Diming Zhang, Yanli Lu, Gang Xu, Yao Yao, Shuang Li, Qingjun Liu, Label-free amino acid detection based on nanocomposites of graphene oxide hybridized with gold nanoparticles, Biosensors and Bioelectronics, 77, 2016, 963-970, https://doi.org/10.1016/j.bios.2015.10.065

- S. Hiren Patel, A. Vishnu Dabhi, M. Aditya Vora, Investigating Electronic, Optical, Thermodynamic, and Thermoelectric Properties of SrO and SrO2 Phases: A Density Functional Theory Approach, ACS Omega 2023, 8, 45, 43008–43023. https://doi.org/10.1021/acsomega.3c06221

- A.u.R. Khan, M. Ramzan, M. Imran, M. Zubair, S. Shahab, S.J. Ahmed, F. Ferreira, M.F. Iqbal. Tailoring the Structural, Optical and Electrical Properties of Zinc Oxide Nanostructures by Zirconium Doping. Coatings. 13(1), 2023, 34. https://doi.org/10.3390/coatings13010034

- V. Mariyappillai, C. Shiyamala, T. Abisheik, M. Tiffany, V. Pandiyan, Adhimoolam Senthilraja, Mohd Afzal, Praveen Barmavatu, Krishnamoorthy Shanmugaraj, Krishnakumar Balu, Zr-modified ZnO nanoparticles: Optimized photocatalytic degradation and antibacterial efficiency for pollution control, Ceramics International, 51(17), 2025, 23003-23020, https://doi.org/10.1016/j.ceramint.2025.02.402.

- D. Boldridge, Morphological Characterization of Fumed Silica Aggregates. Aerosol Science and Technology 44 (3), 2010, 182–86. doi:10.1080/02786820903499462.

- Nagaraj Muthulakshmi, Arumugam Kathirvel, Ramasamy Subramanian, M. Senthil, Biofabrication of Zirconia Nanoparticles: Synthesis, Spectral Characterization and Biological Activity Evaluation against Pathogenic Bacteria, 13(2), 2023, 190 https://doi.org/10.33263/BRIAC132.190

- S. Kavitha, K.S. Mohan, K. Deepika, P.R. Janani, B. Kamali, S. Bhavadharani, The Impact of Zn doping on structural and optical behavior of SrO2 NPs and Anti-Microbial activities for Zn@SrO2 NPs, Materials Today: Proceedings, 94, 2023, 1-12, https://doi.org/10.1016/j.matpr.2023.04.331.

- S. Sultana, Rafiuddin, M. Z. Khan, K. Umar, A. S. Ahmed, M. Shahadat, SnO2–SrO based nanocomposites and their photocatalytic activity for the treatment of organic pollutants, Journal of Molecular Structure, 1098, 2015, 393-399, https://doi.org/10.1016/j.molstruc.2015.06.032.

- V. Mariyappillai, C. Shiyamala, T. Abisheik, M. Tiffany, V. Pandiyan, Adhimoolam Senthilraja, Mohd Afzal, Praveen Barmavatu, Krishnamoorthy Shanmugaraj, Krishnakumar Balu, Zr-modified ZnO nanoparticles: Optimized photocatalytic degradation and antibacterial efficiency for pollution control, Ceramics International, 51(17), 2025, 23003-23020, https://doi.org/10.1016/j.ceramint.2025.02.402.

- N. Raghavendra, H. P. Nagaswarupa, T. R. Shashi Shekhar, M. Mylarappa, N. Basavaraju, B. S. Surendra. Electrochemical Sensor and Photocatalytic Studies of Ferrite Nanoparticle Using Different Fuels via Green Approach, Sensing Technology, 2(1), 2024. doi:10.1080/28361466.2024.2336937.

- G. Hussain, A. Gilane, M. Sohail, D. S. Silvester, Effect of kinetic reversibility on the voltammetric response in room temperature ionic liquids, Electrochimica Acta, 556, 2026, 148396, https://doi.org/10.1016/j.electacta.2026.148396.

- S. Mengxuan, L. Zhijie, L. Hao, W. Zhonglin, S. Wenzhong, F. Yong Qing (Richard), Mesoporous Zr-doped CeO2 nanostructures as superior supercapacitor electrode with significantly enhanced specific capacity and excellent cycling stability. Electrochimica Acta. 331. 2019, 135366. 10.1016/j.electacta.2019.135366.

- M. Holecek, Histidine in Health and Disease: Metabolism, Physiological Importance, and Use as a Supplement. Nutrients, 12(3), 2020, 848. https://doi.org/10.3390/nu12030848

- S.M. Liao, Q.S. Du, J.Z. Meng, Z.W. Pang, R.B. Huang, The multiple roles of histidine in protein interactions. Chemistry Central Journal, 7(1), 2013, 44. doi: 10.1186/1752-153X-7-44.

- S. Jafar Ali Ibrahim, S. Rajasekar, Varsha, M. Karunakaran, K. Kasirajan, N. S. Kalyan Chakravarthy, V. Kumar, K.J. Kaur, Recent advances in performance and effect of Zr doping with ZnO thin film sensor in ammonia vapour sensing, Global NEST Journal, 23(4), 2021, 526-531.